|  | INJECTION MOLDING FLOW ANALYSIS OF SINK MOLD Date: Department: Created by:. Table of Contents Description 1 Machine Information 2 Study Characteristics 2 Injection Unit Settings 3 Polymer Properties 6 Domains 7 Boundary Conditions 8 Global Parameters 10 Mesh Details 11 Fill Results 12 Pack Results 31 Material Parameter 44 X-Y Plot 52 Conclusion: 56. |
| --- | --- |
| # Description |  |

# Machine Information Comments:

| Number of Processors | 8 |
| --- | --- |
| Maximum number of threads | 8 |
| Number of available threads | 8 |
| Software type | Windows 10 |
| SOLIDWORKS Plastics version | SOLIDWORKS Plastics Premium 2025 SP1.0 |

# Study Characteristics Comments:

| Part name | Sink Design solidworks |
| --- | --- |
| Configuration | Default |
| Study Name | FLOW ANALYSIS |
| Injection Process | Single Material |
| Number of Injection Units | 1 |
| Analysis (Mesh) Procedure | Solid |
| Simulation Type | Fill + Pack |

# Injection Unit Settings ## Unit 1

| Material | Generic material / Generic PP |
| --- | --- |
| Filling Time | Automatic |
| Melt Temperature | 230 °C |
| Mold temperature | 50 °C |
| Injection Pressure Limit | 100 MPa |
| Fill/Pack Switch Point (% Filled Volume) | 100 % |
| Temperature Criteria for Short Shots | 135°C |
| Mold Temperature Profile | Off |
| Mold-Melt Heat Transfer Coefficient | Off |
| Pressure Holding Time | Automatic |
| Pure Cooling Time | 80 sec |

Flow Rate Profile Setting:

Time control (Relative control)/Base on filling time

Pressure Profile Setting:

Relative to pressure at filling end (Relative control)

# Polymer Properties

Generic material / Generic PP Ejection Temperature; 95°C. Transition Temperature; 135°C. Young Modulus; E1: 1350 MPa, E2: 1350 MPa. Poisson's Ratio; v12: 0.4, v23: 0.4. Max. Shear Rate; 100000 1/s. Max. Shear Stress; 0.25 MPa. Fiber Percentage; Not Available.

# Domains

| Name | Image |
| --- | --- |
| Combine2 (-Cavity-) |  |

# Boundary Conditions

| Name | Boundary Condition Image | Details |
| --- | --- | --- |
| Injection Location-1 |  | Entity name:. |

| Name | Boundary Condition Image | Details |
| --- | --- | --- |
| Clamp Force-1 |  | Clamp Force Direction:. Excluded Region:. |

| Name | Boundary Condition Image | Details |
| --- | --- | --- |
| Air Vents-1 |  | Entity name:. |

# Global Parameters

General Clamp Force Limit; 100 Tonne. Ambient Temperature; 30 °C.

Fill-Pack Gravity Downward Direction for fill; -Y. Venting Analysis; Off. Solver Type; AMG. Volume of Fluid Algorithm; CICSAM.

Warp Gravity Downward Direction for warp; -Y. Solver Type; AMG.

Cool Mold Open Time; 5 sec. Specify control based on <Ejection Temperature /Cooling Time >; Ejection Temperature. Solver Type; AMG. Analysis Method; FEM-Linear.

# Mesh Details

# Fill Results

Comments:

## Fill Summary

| Clamp Force | 2.4426 Tonne |
| --- | --- |
| X-dir. Clamping Force | 1.1999 Tonne |
| Y-dir. Clamping Force | 2.4426 Tonne |
| Z-dir. Clamping Force | 1.2252 Tonne |
| Required injection pressure | 8.3592 Mpa |
| Max. real temperature | 230.1567 °C |
| Max. bulk temperature | 230.1565 °C |
| Max. shear stress | 0.2409 Mpa |
| Max. shear rate | 2883.3990 1/sec |
| CPU Time | 717.59 sec |
| Cycle Time | 115.16 sec |
| 1. Filling Time | 10.16 sec |
| 2. Total Time in Pack Stage | 100.00 sec |
| a). Pressure Holding Time | 20.27 sec |
| b). Pure Cooling Time | 79.73 sec |
| 3. Mold Open Time | 5.00 sec |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Fill Time | Fill Results | 0.010087 | 10.155290 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Pressure at End of Fill | Fill Results | 0.102751 | 8.359222 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Temperature at End of Fill | Fill Results | 66.380928 | 230.006699 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Bulk Temperature at End of Fill | Fill Results | 66.455360 | 230.006500 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Flow Front Temperature | Fill Results | 178.105698 | 229.900696 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Temperature Growth at End of Fill | Fill Results | 0.000000 | 0.006468 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Shear Stress at End of Fill | Fill Results | 0.000080 | 0.240875 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Shear Rate at End of Fill | Fill Results | 0.025106 | 2883.398926 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Volumetric Shrinkage at End of Fill | Fill Results | 4.067349 | 17.270281 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Freezing Time at End of Fill | Fill Results | 1.953608 | 10.154260 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Cooling Time | Fill Results | 10.355290 | 816.155273 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Temperature at End of Cooling | Fill Results | 49.999962 | 168.626495 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Frozen Area at End of Fill | Fill Results | 0.000000 | 1.000000 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Velocity Vector at End of Fill | Fill Results | 0.000022 | 100.619127 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Gate Filling Contribution | Fill Results | 0.000000 | 1.000000 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Ease of Fill | Fill Results | 0.000000 | 2.000000 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Weld Lines | Fill Results | 3.490000 | 147.910004 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Air Traps | Fill Results | 0.010087 | 10.155290 |

# Pack Results

Comments:

## Pack Summary

| Clamp Force | 29.5291 Tonne |
| --- | --- |
| X-dir. Clamping Force | 14.3119 Tonne |
| Y-dir. Clamping Force | 29.5291 Tonne |
| Z-dir. Clamping Force | 14.7500 Tonne |
| Max. real temperature | 229.3655 °C |
| Max. bulk temperature | 230.0257 °C |
| Max. shear stress | 0.3484 Mpa |
| Max. shear rate | 0.3235 1/sec |
| Max. residual stress | 59.1820 Mpa |
| Mass at the end of packing | 502.88 (g) |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Pressure at End of Packing | Pack Results | 0.100000 | 3.404000 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Temperature at End of Packing | Pack Results | 54.794930 | 229.835205 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Bulk Temperature at End of Packing | Pack Results | 55.030510 | 229.875702 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Density at End of Packing | Pack Results | 0.787553 | 0.945057 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Shear Stress at End of Packing | Pack Results | 0.000087 | 0.348427 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Shear Rate at End of Packing | Pack Results | 0.000157 | 0.323529 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Volumetric Shrinkage at End of Packing | Pack Results | 2.017585 | 17.734529 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Temperature at Post-Filling End | Pack Results | 50.119011 | 229.215500 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Freezing Time at Post-Filling End | Pack Results | 1.953608 | 107.925301 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Residual Stress at Post-Filling End | Pack Results | 4.123033 | 59.182018 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Sink Marks at Ejection | Pack Results | 0.000000 | 1.118917 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Frozen Area at Post-Filling End | Pack Results | 0.000000 | 1.000000 |

# Material Parameter

Comments:

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Polymer Viscosity Graph | Material Parameter |  |  |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Polymer Specific-Volume Graph | Material Parameter |  |  |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Polymer Specific-Heat Graph | Material Parameter |  |  |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Polymer Thermal-Conductivity Graph | Material Parameter |  |  |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Polymer Elastic-Modulus Graph | Material Parameter |  |  |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Polymer Poisson-Ratio Graph | Material Parameter |  |  |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Polymer Linear-Thermal-Expansion-Coefficient Graph | Material Parameter |  |  |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Polymer Relaxation-Modulus Graph | Material Parameter |  |  |

# X-Y Plot

Comments:

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Max. Injection Pressure | X-Y Plot | 0.000000 | 8.266000 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Melt Front Flow Rate | X-Y Plot | -65.820000 | 65.669998 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Clamp Force | X-Y Plot | 0.000000 | 29.528999 |

| Name | Type | Min | Max |
| --- | --- | --- | --- |
| Part Mass | X-Y Plot | 0.000000 | 502.882996 |

# Conclusion: