## Slide 1
INJECTION MOLDING FLOW ANALYSIS OF SINK MOLD
<Study_Image/>
Date | 
Created by | 
Department | 
Organization | 
Logo | 
URL | 

## Slide 2
Description

## Slide 3
Machine Information
Number of Processors | 8
Maximum number of threads | 8
Number of available threads | 8
Software type | Windows 10
SOLIDWORKS Plastics version | SOLIDWORKS Plastics Premium 2025 SP1.0

## Slide 4
Study Characteristics
Part name | Sink Design solidworks
Configuration | Default
Study Name | FLOW ANALYSIS
Injection Process | Single Material
Number of Injection Units | 1
Analysis (Mesh) Procedure | Solid
Simulation Type | Fill + Pack

## Slide 5
Injection Unit 1 Settings
Material | Generic material / Generic PP
Filling Time | Automatic
Melt Temperature | 230 °C
Mold temperature | 50 °C
Injection Pressure Limit | 100 MPa
Fill/Pack Switch Point (% Filled Volume) | 100 %
Temperature Criteria for Short Shots | 135°C
Mold Temperature Profile | Off
Mold-Melt Heat Transfer Coefficient | Off
Pressure Holding Time | Automatic
Pure Cooling Time | 80 sec

## Slide 6
Polymer Properties
Trade Name and Grade: Generic material / Generic PP
Ejection Temperature | 95°C
Transition Temperature | 135°C
Young Modulus | E1: 1350 MPa, E2: 1350 MPa
Poisson's Ratio | v12: 0.4, v23: 0.4
Max. Shear Rate | 100000 1/s
Max. Shear Stress | 0.25 MPa
Fiber Percentage | Not Available

## Slide 7
Domains
Name | Image
Combine2 (-Cavity-) | 

## Slide 8
Boundary Conditions
Name | Image | Details | 
Injection Location-1 |  | Entity name | 

## Slide 9
Name | Image | Details | 
Clamp Force-1 |  | Clamp Force Direction | 
 |  | Excluded Region | 
Boundary Conditions

## Slide 10
Name | Image | Details | 
Air Vents-1 |  | Entity name | 
Boundary Conditions

## Slide 11
Global Parameters
General
Clamp Force Limit: 100 Tonne Ambient Temperature: 30 °C

## Slide 12
Global Parameters
Fill-Pack
Gravity Downward Direction for fill: -Y Venting Analysis: Off Solver Type: AMG Volume of Fluid Algorithm: CICSAM

## Slide 13
Global Parameters
Warp
Gravity Downward Direction for warp: -Y Solver Type: AMG

## Slide 14
Global Parameters
Cool
Mold Open Time: 5 sec Specify control based on <Ejection Temperature /Cooling Time >: Ejection Temperature Solver Type: AMG Analysis Method: FEM-Linear

## Slide 15
Mesh Details
<Image_Mesh_Details/>

## Slide 16
Results Summary
<Results_Summary/>
Fill Results
Clamp Force | 2.4426 Tonne
X-dir. Clamping Force | 1.1999 Tonne
Y-dir. Clamping Force | 2.4426 Tonne
Z-dir. Clamping Force | 1.2252 Tonne
Required injection pressure | 8.3592 Mpa
Max. real temperature | 230.1567 °C
Max. bulk temperature | 230.1565 °C
Max. shear stress | 0.2409 Mpa
Max. shear rate | 2883.3990 1/sec

## Slide 17
Results Summary
<Results_Summary/>
Fill Results
CPU Time | 717.59 sec
Cycle Time | 115.16 sec
1. Filling Time | 10.16 sec
2. Total Time in Pack Stage | 100.00 sec
a). Pressure Holding Time | 20.27 sec
b). Pure Cooling Time | 79.73 sec
3. Mold Open Time | 5.00 sec

## Slide 18
Filling Animation
<Image_Res>

## Slide 19
Fill Time
<Image_Res>

## Slide 20
Pressure at End of Fill
<Image_Res>

## Slide 21
Temperature at End of Fill
<Image_Res>

## Slide 22
Bulk Temperature at End of Fill
<Image_Res>

## Slide 23
Flow Front Temperature
<Image_Res>

## Slide 24
Temperature Growth at End of Fill
<Image_Res>

## Slide 25
Shear Stress at End of Fill
<Image_Res>

## Slide 26
Shear Rate at End of Fill
<Image_Res>

## Slide 27
Volumetric Shrinkage at End of Fill
<Image_Res>

## Slide 28
Freezing Time at End of Fill
<Image_Res>

## Slide 29
Cooling Time
<Image_Res>

## Slide 30
Temperature at End of Cooling
<Image_Res>

## Slide 31
Frozen Area at End of Fill
<Image_Res>

## Slide 32
Velocity Vector at End of Fill
<Image_Res>

## Slide 33
Gate Filling Contribution
<Image_Res>

## Slide 34
Ease of Fill
<Image_Res>

## Slide 35
Weld Lines
<Image_Res>

## Slide 36
Air Traps
<Image_Res>

## Slide 37
Results Summary
<Results_Summary/>
Pack Results
Clamp Force | 29.5291 Tonne
X-dir. Clamping Force | 14.3119 Tonne
Y-dir. Clamping Force | 29.5291 Tonne
Z-dir. Clamping Force | 14.7500 Tonne
Max. real temperature | 229.3655 °C
Max. bulk temperature | 230.0257 °C
Max. shear stress | 0.3484 Mpa
Max. shear rate | 0.3235 1/sec
Max. residual stress | 59.1820 Mpa
Mass at the end of packing | 502.88 (g)

## Slide 38
Pressure at End of Packing
<Image_Res>

## Slide 39
Temperature at End of Packing
<Image_Res>

## Slide 40
Bulk Temperature at End of Packing
<Image_Res>

## Slide 41
Density at End of Packing
<Image_Res>

## Slide 42
Shear Stress at End of Packing
<Image_Res>

## Slide 43
Shear Rate at End of Packing
<Image_Res>

## Slide 44
Volumetric Shrinkage at End of Packing
<Image_Res>

## Slide 45
Temperature at Post-Filling End
<Image_Res>

## Slide 46
Freezing Time at Post-Filling End
<Image_Res>

## Slide 47
Residual Stress at Post-Filling End
<Image_Res>

## Slide 48
Sink Marks at Ejection
<Image_Res>

## Slide 49
Frozen Area at Post-Filling End
<Image_Res>

## Slide 50
X-Y Plot
Material Parameter
<Image_Res>

## Slide 51
X-Y Plot
Material Parameter
<Image_Res>

## Slide 52
X-Y Plot
Material Parameter
<Image_Res>

## Slide 53
X-Y Plot
Material Parameter
<Image_Res>

## Slide 54
X-Y Plot
Material Parameter
<Image_Res>

## Slide 55
X-Y Plot
Material Parameter
<Image_Res>

## Slide 56
X-Y Plot
Material Parameter
<Image_Res>

## Slide 57
X-Y Plot
Material Parameter
<Image_Res>

## Slide 58
X-Y Plot
Max. Injection Pressure
<Image_Res>

## Slide 59
X-Y Plot
Melt Front Flow Rate
<Image_Res>

## Slide 60
X-Y Plot
Clamp Force
<Image_Res>

## Slide 61
X-Y Plot
Part Mass
<Image_Res>

## Slide 62
Conclusion